## Slide 1: Introduction
Phase: A region in a material that differs in structure and function from other regions.
Phase diagrams:
    Represents phases present in metal at different conditions (Temperature, pressure and composition).
    Indicates equilibrium solid solubility of one element in another.
    Indicates temperature range under which solidification occurs.
    Indicates temperature at which different phases start to melt.

## Slide 2: Phase Diagram of Pure Substances
Pure substance exist as solid, liquid and vapor.
Phases are separated by phase boundaries.
Example : Water, Pure Iron.
Different phases coexist at triple point.
After W. G. Moffatt, et al., “The Structure and Properties of Materials,” vol I: “Structure,” Wiley, 1965, p.151
BCC
BCC
FCC

## Slide 3: Phase Diagrams & The Equilibrium Constitution of an Alloy
Key Features
  Axes: Composition and Temperature
  Regions Labeled with the Names of Materials
  Lines that Separate the Regions
  Points Where the Lines Intersect
Key Uses are to Predict
  Which Phases Are Present in an Alloy (Mixture)
  How Much of Each
  The Microstructure

## Slide 4: Phase Fields for Binary Alloys
Conventions
  “A” and “B” are the generic Components
  Is a solid solution in which A is the solvent and B is the solute
    has A’s Crystal structure
  b Is a solid solution in which B is the solvent and A is the solute
    has B’s Crystal structure
  Other Greek letters are compounds formed from A & B
“A”
“B”
Single Phase and 2-Phase “Phase Fields”
  Pure Components (Lines at limits of the Phase Diagram
  Solutions
  Mixtures of a Liquid & Solid, 2 Different Solids, 2 Different Liq’ds

## Slide 5: How to Read A Binary Phase Diagram
Phases Present
  Determine the Constitution Point (CB,T)
    CB represents the ingredients; T is the temperature
  Phases Present are Given by the Field in Which the Constitution Point Lies

## Slide 6: Composition of the Phases Present
Single Phase Field
  Only Have One Phase
  Phase composition Must Equal Alloy Composition
Liquid
L +
a + b
L +
a
b
a
A
B
W
B in the alloy
A vs. a, B vs. b
  A, B are the Pure Components
  a is “A” with some B Dissolved in It
    Same Crystal Structure as Pure A
    Some A Atoms Replaced with B atoms
b

## Slide 7: Composition of the Phases Present
Two-Phase Field
  Two Phases
  Phase Compositions Are @ the Solubility Limits
  Tie-Line Construction Gives Phase Compositions
Tie Line Construction
  Draw a Line of Constant T at T of Interest
  Phase Composition = Composition Where Tie Line Intersects the Phase Field Boundaries
    WHY? (Gives the Solubility Limit at T of Interest!)
Liquid
L +
L +
a + b
a
b
b
a
A
B
W
W
B in grains
a
B in grains
b
W
B in the alloy

## Slide 8: For a Real Phase Diagram
Single Phase Field, Alloy #1
  Only Have one Phase
  Phase Composition Must Equal Alloy Composition
Two-Phase Field, Alloy #2
  Two Phases
  Phase Compositions Are @ Solubility Limits
  Tie-Line Construction Gives Phase Compositions
  Note: At Constant T, the Composition of a and b in the Two Phase Field Do NOT Vary with Alloy Composition!
    Why?
Wt% Sn in a
Wt% Sn in b
Alloy #2 Composition
Wt%Sn in a
Alloy #1 Composition

## Slide 9: Gibbs Phase Rule
P+F = C+2
For pure water, at triple point, 3 phases coexist.
There is one component (water) in the system.
Therefore 3 + F = 1 + 2 F = 0.
Degrees of freedom indicate number of variables that can be changed without changing number of phases.
P = number of phases that coexist in a system
C = Number of components
F = Degrees of freedom

## Slide 10: Components and Phases
• Components:
The elements or compounds which are present in the alloy
(e.g., Al and Cu)
• Phases:
The physically and chemically distinct material regions
that form (e.g., a and b).
Aluminum-
Copper
Alloy
a
(darker
phase)
b
(lighter
phase)
Adapted from chapter-opening photograph, Chapter 9, Callister, Materials Science & Engineering: An Introduction, 3e.

## Slide 11: Criteria for Solid Solubility
 | Crystal Structure | electroneg | r (nm)
Ni | FCC | 1.9 | 0.1246
Cu | FCC | 1.8 | 0.1278
Both have the same crystal structure (FCC) and have similar electronegativities and atomic radii (W. Hume – Rothery rules) suggesting high mutual solubility.
Simple system (e.g., Ni-Cu solution)
Ni and Cu are totally soluble in one another for all proportions.

## Slide 12: Complete Solid Solubility
Complete Solid Solubility
  Get only one solid (solution) for All Alloy Compositions, WB
  Components Must Be “Similar (At minimum, same crystal structure)
Definitions
Liquidus Line
  Line above which the alloy is all liquid
Solidus Line
  Line below which the alloy is all solid
Can give the liquidus and solidus temperature for any alloy composition
Classic Example: Cu-Ni

## Slide 13: Isomorphous Binary Phase Diagram
13
Cu-Ni
phase
diagram
• Phase diagram:
Cu-Ni system.
• System is:
Adapted from Fig. 10.3(a), Callister & Rethwisch 3e. (Fig. 10.3(a) is adapted from Phase Diagrams of Binary Nickel Alloys, P. Nash (Ed.), ASM International, Materials Park, OH (1991).
-- binary
i.e., 2 components:
Cu and Ni.
-- isomorphous
i.e., complete
solubility of one
component in
another; a phase
field extends from
0 to 100 wt% Ni.
wt% Ni
20
40
60
80
100
0
1000
1100
1200
1300
1400
1500
1600
T(°C)
L (liquid)
a
(FCC solid
solution)
L
+
a
liquidus
solidus
Notes: 13

## Slide 14: Binary Isomorphous Alloy Systems
Binary alloy
Isomorphous system: Two elements completely soluble in each other in liquid and solid state.
Example: Cu-Ni solution.
Mixture of
two systems
Two component
system
Composition at liquid
and solid phases at any
temperature can be
determined by drawing
a tie line.
Adapted from “Metals Handbook,” vol. 8, 8th ed., American society of Metals, 1973, p. 294.

## Slide 15: Phase Diagrams: Determination of phase(s) present
wt% Ni
20
40
60
80
100
0
1000
1100
1200
1300
1400
1500
1600
T(°C)
L (liquid)
a
(FCC solid solution)
L
+
a
liquidus
solidus
15
• Rule 1: If we know T and Co, then we know:
-- which phase(s) is (are) present.
• Examples:
A(1100°C, 60 wt% Ni):
1 phase: a
B
(1250°C, 35 wt% Ni):
2 phases: L + a
B
(1250°C,35)
A(1100°C,60)
Adapted from Fig. 10.3(a), Callister & Rethwisch 3e. (Fig. 10.3(a) is adapted from Phase Diagrams of Binary Nickel Alloys, P. Nash (Ed.), ASM International, Materials Park, OH (1991).
Notes: 15

## Slide 16: Phase Diagrams: Determination of phase compositions
16
wt% Ni
20
1200
1300
T(°C)
L (liquid)
a
(solid)
L
+
a
liquidus
solidus
30
40
50
L
+
a
Cu-Ni system
• Rule 2: If we know T and C0, then we can determine:
-- the composition of each phase.
• Examples:
TA
A
35
C0
32
CL
At TA
= 1320°C:
Only Liquid (L) present
CL = C0
( = 35 wt% Ni)
At TB
= 1250°C:
Both

and L present
CL
= C
liquidus
( = 32 wt% Ni)
C
= C
solidus
( = 43 wt% Ni)
At TD
= 1190°C:
Only Solid (a) present
C = C0
( = 35 wt% Ni)
Consider C0 = 35 wt% Ni
D
TD
tie line
4
C
3
Adapted from Fig. 10.3(a), Callister & Rethwisch 3e. (Fig. 10.3(a) is adapted from Phase Diagrams of Binary Nickel Alloys, P. Nash (Ed.), ASM International, Materials Park, OH (1991).
B
TB
Notes: 16

## Slide 17: The Lever Rule
The Lever rule gives the weight % of phases in any two phase regions.
Wt fraction of solid phase
= Xs = w0 – wl
ws – wl
Wt fraction of liquid phase
= Xl = ws – w0
ws – wl

## Slide 18: Binary Eutectic Alloy System
In some binary alloy systems, components have limited solid solubility.
Eutectic composition freezes
at lower temperature than all
other compositions.
This lowest temperature is
called eutectic temperature.
Liquid
α solid solution + β solid solution
Eutectic temperature
Cooling
Example : Pb-Sn alloy.
Lead
-Tin

## Slide 19: EX : Pb-Sn Eutectic System
19
L
+
a
L
+
b
a
+
b
200
T(°C)
18.3
C, wt% Sn
20
60
80
100
0
300
100
L (liquid)
a
183°C
61.9
97.8
b
• For a 40 wt% Sn-60 wt% Pb alloy at 150°C, determine:
-- the phases present
Pb-Sn
system
Answer: a + b
-- the phase compositions
-- the relative amount of each phase
150
40
C0
11
C
99
C
S
R
Answer: Ca = 11 wt% Sn
Cb = 99 wt% Sn
W

=
C - C0
C - C
=
99 - 40
99 - 11
=
59
88
= 0.67
S
R+S
=
W

=
C0 - C
C - C
=
R
R+S
=
29
88
= 0.33
=
40 - 11
99 - 11
Answer:
Adapted from Fig. 10.8, Callister & Rethwisch 3e.
Notes: 19

## Slide 20: Microstructural Developments in Eutectic Systems I
20
• For alloys for which
C0 < 2 wt% Sn
• Result: at room temperature
-- polycrystalline with grains of
a phase having
composition C0
0
L
+
a
200
T(°C)
C
,
wt% Sn
10
2
20
C0
300
100
L
a
30
a
+
b
400
(room T solubility limit)
TE
(Pb-Sn
System)
a
L
L: C0 wt% Sn
a: C0 wt% Sn
Adapted from Fig. 10.11, Callister & Rethwisch 3e.
Notes: 20

## Slide 21: Microstructural Developments in Eutectic Systems II
21
• For alloys for which
2 wt% Sn < C0 < 18.3 wt% Sn
• Result:
at temperatures in a + b range
-- polycrystalline with a grains
and small b-phase particles
Adapted from Fig. 10.12, Callister & Rethwisch 3e.
Pb-Sn
system
L
+
a
200
T(°C)
C
,
wt% Sn
10
18.3
20
0
C0
300
100
L
a
30
a
+
b
400
(sol. limit at TE)
TE
2
(sol. limit at T
room
)
L
a
L: C0 wt% Sn
a
b
a: C0 wt% Sn
Notes: 21

## Slide 22: Microstructural Developments in Eutectic Systems III
22
• For alloy of composition C0 = CE
• Result: Eutectic microstructure (lamellar structure)
-- alternating layers (lamellae) of a and b phases.
Adapted from Fig. 10.13, Callister & Rethwisch 3e.
Adapted from Fig. 10.14, Callister & Rethwisch 3e.
160 m
Micrograph of Pb-Sn
eutectic
microstructure
Pb-Sn
system
L
a
200
T(°C)
C, wt% Sn
20
60
80
100
0
300
100
L
a
b
L
+
a
183°C
40
TE
18.3
: 18.3 wt%Sn
97.8
: 97.8 wt% Sn
CE
61.9
L: C0 wt% Sn
Notes: 22

## Slide 23: Microstructural Developments in Eutectic Systems IV
23
• For alloys for which 18.3 wt% Sn < C0 < 61.9 wt% Sn
• Result: a phase particles and a eutectic microconstituent
18.3
61.9
S
R
97.8
S
R
primary
a
eutectic
a
eutectic
b
WL
= (1-
W
a
)
= 0.50
Ca
= 18.3 wt% Sn
CL
= 61.9 wt% Sn
S
R
+
S
Wa
=
= 0.50
• Just above TE :
• Just below TE :
C

= 18.3 wt% Sn
C

= 97.8 wt% Sn
S
R
+
S
W

=
= 0.73
W

= 0.27
Adapted from Fig. 10.16, Callister & Rethwisch 3e.
Pb-Sn
system
L
+

200
T(°C)
C, wt% Sn
20
60
80
100
0
300
100
L
a
b
L
+

40

+

TE
L: C0
wt% Sn
L

L

Notes: 23

## Slide 24: Eutectic, Eutectoid, & Peritectic
24
Eutectoid – one solid phase transforms to two other solid phases
  S2 S1+S3
    + Fe3C (For Fe-C, 727C, 0.76 wt% C)
intermetallic compound - cementite
cool
heat
Eutectic - liquid transforms to two solid phases
  L  +  (For Pb-Sn, 183C, 61.9 wt% Sn)
cool
heat
cool
heat
Peritectic - liquid and one solid phase transform to a second solid phase
  S1 + L S2
   + L  (For Fe-C, 1493°C, 0.16 wt% C)
Notes: 24

## Slide 25: Hypoeutectic & Hypereutectic
25
L
+
a
L
+
b
a
+
b
200
C, wt% Sn
20
60
80
100
0
300
100
L
a
b
TE
40
(Pb-Sn
System)
Adapted from Fig. 10.8,
Callister & Rethwisch 3e. (Fig. 10.8 adapted from Binary Phase Diagrams, 2nd ed., Vol. 3, T.B. Massalski (Editor-in-Chief), ASM International, Materials Park, OH, 1990.)
160 mm
eutectic micro-constituent
Adapted from Fig. 10.14, Callister & Rethwisch 3e.
hypereutectic: (illustration only)
b
b
b
b
b
b
Adapted from Fig. 10.17, Callister & Rethwisch 3e. (Illustration only)
(Figs. 10.14 and 10.17 from Metals Handbook, 9th ed.,
Vol. 9, Metallography and Microstructures, American Society for Metals, Materials Park, OH, 1985.)
175 mm
a
a
a
a
a
a
hypoeutectic: C0 = 50 wt% Sn
Adapted from
Fig. 10.17, Callister & Rethwisch 3e.
T(°C)
61.9
eutectic
eutectic: C0 = 61.9 wt% Sn
Notes: 25

## Slide 26: Eutectoid & Peritectic
26
Cu-Zn Phase diagram
Adapted from Fig. 10.21, Callister & Rethwisch 3e.
Eutectoid transformation   + 
Peritectic transformation  + L 
Notes: 26

## Slide 27: Hypoeutectoid Steel
27
Fe3C (cementite)
1600
1400
1200
1000
800
600
400
0
1
2
3
4
5
6
6.7
L
g
(austenite)
g
+L
g
+ Fe3C
a
+ Fe3C
L+Fe3C
d
(Fe)
C, wt% C
1148°C
T(°C)
a
727°C
(Fe-C
System)
C0
0.76
Adapted from Figs. 10.28 and 10.33,Callister & Rethwisch 3e.
(Fig. 10.28 adapted from Binary Alloy Phase Diagrams, 2nd ed., Vol. 1, T.B. Massalski (Ed.-in-Chief), ASM International, Materials Park, OH, 1990.)
Adapted from Fig. 10.34, Callister & Rethwisch 3e.
proeutectoid ferrite
pearlite
100 mm
Hypoeutectoid
steel
a
pearlite
g
g
g
g
a
a
a
g
g
g
g
g
g
g
g
Notes: 27

## Slide 28: Hypoeutectoid Steel
28
Fe3C (cementite)
1600
1400
1200
1000
800
600
400
0
1
2
3
4
5
6
6.7
L
g
(austenite)
g
+L
g
+ Fe3C
a
+ Fe3C
L+Fe3C
d
(Fe)
C, wt% C
1148°C
T(°C)
a
727°C
(Fe-C
System)
C0
0.76
g
g
g
g
a
a
a
s
r
Wa = s/(r + s)
Wg =(1 - Wa)
R
S
a
pearlite
Wpearlite = Wg
Wa’ = S/(R + S)
W =(1 – Wa’)
Fe3C
Adapted from Figs. 10.28 and 10.33,Callister & Rethwisch 3e.
(Fig. 10.28 adapted from Binary Alloy Phase Diagrams, 2nd ed., Vol. 1, T.B. Massalski (Ed.-in-Chief), ASM International, Materials Park, OH, 1990.)
Adapted from Fig. 10.34, Callister & Rethwisch 3e.
proeutectoid ferrite
pearlite
100 mm
Hypoeutectoid
steel
Notes: 28

## Slide 29: Hypereutectoid Steel
29
Fe3C (cementite)
1600
1400
1200
1000
800
600
400
0
1
2
3
4
5
6
6.7
L
g
(austenite)
g
+L
g
+Fe3C
a
+Fe3C
L+Fe3C
d
(Fe)
C, wt%C
1148°C
T(°C)
a
Adapted from Figs. 10.28 and 10.36,Callister & Rethwisch 3e. (Fig. 10.28 adapted from Binary Alloy Phase Diagrams, 2nd ed., Vol. 1, T.B. Massalski (Ed.-in-Chief), ASM International, Materials Park, OH, 1990.)
(Fe-C
System)
0.76
C0
Fe3C
g
g
g
g
g
g
g
g
g
g
g
g
Adapted from Fig. 10.37, Callister & Rethwisch 3e.
proeutectoid Fe3C
60 mm
Hypereutectoid
steel
pearlite
pearlite
Notes: 29

## Slide 30: Hypereutectoid Steel
30
Fe3C (cementite)
1600
1400
1200
1000
800
600
400
0
1
2
3
4
5
6
6.7
L
g
(austenite)
g
+L
g
+Fe3C
a
+Fe3C
L+Fe3C
d
(Fe)
C, wt%C
1148°C
T(°C)
a
(Fe-C
System)
0.76
C0
pearlite
Fe3C
g
g
g
g
x
v
V
X
Wpearlite = Wg
Wa = X/(V + X)
W =(1 - Wa)
Fe3C’
W =(1-Wg)
Wg =x/(v + x)
Fe3C
Adapted from Fig. 10.37, Callister & Rethwisch 3e.
proeutectoid Fe3C
60 mm
Hypereutectoid
steel
pearlite
Adapted from Figs. 10.28 and 10.36,Callister & Rethwisch 3e. (Fig. 10.28 adapted from Binary Alloy Phase Diagrams, 2nd ed., Vol. 1, T.B. Massalski (Ed.-in-Chief), ASM International, Materials Park, OH, 1990.)
Notes: 30

## Slide 31: Various Eutectic Structures
Structure depends on factors like minimization of free energy at α / β interface.
Manner in which two phases nucleate and grow also affects structures.
After W. C. Winegard, “An Introduction to the Solidification of Metals,” Institute of Metals, London, 1964.

## Slide 32: Binary Peritectic Alloy System
Peritectic reaction: Liquid phase reacts with a solid phase to form a new and different solid phase.
Liquid + α β
cooling
Peritectic reaction occurs
when a slowly cooled alloy
of Fe-4.3 wt% Ni passes
through Peritectic
temperature of 15170C.
Peritectic point is invariant.
Liquid(5.4 wt% Ni) + δ (4.0 wt% Ni) γ 4.3 wt % Ni
cooling

## Slide 33: Peritectic Alloy System
At 42.4 % Ag & 14000C
Phases present Liquid Alpha
Composition 55% Ag 7%Ag
Amount of Phases 42.4 –7 55-42.4
55 – 7 55 - 7
= 74% = 26%
At 42.4% Ag and 11860C – ΔT
Phase Present Beta only
Composition 42.4% Ag
Amount of Phase 100%
At 42.4% Ag and 11860C + ΔT
Phases present Liquid Alpha
Composition 66.3% Ag 10.5%Ag
Amount of Phases 42.4 –10.5 66.3-42.4
66.3 – 10.5 66.3–10.5
= 57% =43%